## Slide 1
PRACTICAL ENGINEERING TOOLKIT
INJECTION MOULD
DESIGN & CALCULATIONS
A–Z formulas • worked examples • design checks
For students, junior designers and manufacturing professionals
EDUCATIONAL EDITION | SI UNITS
MOULD • MATERIAL • PROCESS

## Slide 2
How to use this toolkit
START HERE
02
01 Learn the formula
Each calculation includes the purpose, equation and required inputs.
02 Follow the example
Worked examples use illustrative values and SI units.
03 Verify the design
Confirm results with CAD, material data, machine limits and trials.
Scope: conventional thermoplastic injection moulding. This is a practical reference—not a substitute for a mould-flow study, detailed mechanical design, supplier data or a qualified engineering review.
All numerical values are examples unless explicitly identified as a standard or supplier specification.

## Slide 3
A–Z mould calculation workflow
DESIGN PROCESS
03
01 Part data
Collect drawing, volume, wall thickness and quality needs
02 Material & shrinkage
Use grade-specific supplier data
03 Cavity count
Balance productivity, cost and machine limits
04 Projected area & clamp
Use projected area at the parting line
05 Shot & machine fit
Check shot volume, pressure and tie-bar spacing
06 Runner / gate
Balance flow length, pressure drop and filling
07 Cooling
Estimate heat load and channel performance
08 Ejection / venting
Check release, draft, vents and safe ejection
09 Steel & tolerances
Choose steel and tolerances for life and accuracy
10 Trials & validation
Measure parts and optimise process window

## Slide 4
Start with reliable input data
PART & MATERIAL DATA
04
• 3D CAD model and 2D drawing with critical dimensions
• Part volume, mass, projected area and maximum flow length
• Nominal wall thickness, ribs, bosses, holes and undercuts
• Resin grade, density, shrinkage range and processing window
• Surface finish, appearance, tolerance and annual demand
• Machine: shot capacity, injection pressure, clamp force
• Tie-bar spacing, platen size, daylight and ejector stroke
• Cavity count, runner type and gate concept
• Cooling-water temperature, flow and available connections
• Production constraints, safety factors and validation plan
Rule: do not calculate from a screenshot alone when the CAD model, resin grade or machine data is available.

## Slide 5
1. Mould shrinkage & cavity dimensions
DIMENSIONING
05
Basic formula
Mould dimension ≈ finished-part dimension ÷ (1 − shrinkage fraction)
Use the material supplier's definition and shrinkage data.
Example
Finished dimension = 100.00 mm
Assumed linear shrinkage = 1.5% = 0.015
Mould dimension ≈ 100 ÷ 0.985 = 101.52 mm
Important: shrinkage is not a universal constant. It varies with resin grade, glass/mineral fill, flow direction, wall thickness, packing pressure, gate location, mould temperature and part geometry.
For filled polymers, anisotropic shrinkage and warpage may require simulation and measured tool corrections.

## Slide 6
2. Part volume & shot mass
MATERIAL ESTIMATION
06
Part mass
Mass (g) = Volume (cm³) × Density (g/cm³)
Example: 42 cm³ × 1.05 g/cm³ = 44.1 g per part
Total shot mass
Shot mass ≈ (part mass × cavity count) + runner / sprue mass
Example: 4 × 44.1 g + 18 g runner = 194.4 g
Use CAD volume for complex geometry. Density must match the exact resin grade and conditioning basis. Hot-runner systems may reduce or eliminate cold-runner mass but still require a validated shot-size check.
Do not confuse theoretical shot capacity with the machine's usable process window.

## Slide 7
3. Projected area & clamp force
MACHINE SIZING
07
Projected area
Use the silhouette projected onto the parting plane.
For a rectangle: A = length × width
For complex parts: use CAD projection.
Clamp force estimate
Clamp force ≈ total projected area × cavity pressure
Keep units consistent: cm² × MPa → force in N after conversion.
Quick unit relation: 1 MPa = 1 N/mm². Therefore, if area is in mm² and cavity pressure is in MPa, force in N = area × pressure. Divide by 1,000 to obtain kN; divide kN by 9.80665 for metric tonnes-force.
Include all cavities and runner area that contribute to parting-line opening force.

## Slide 8
4. Worked example: clamp tonnage
MACHINE SIZING
08
Given
4 cavities
Projected area / part = 80 cm²
Assumed average cavity pressure = 35 MPa
Total area
4 × 80 = 320 cm²
320 cm² = 32,000 mm²
Force = 32,000 × 35 = 1,120,000 N
Result
1,120 kN ≈ 114 metric tonnes-force
Apply a justified process/design margin and verify against actual cavity pressure.
This is an illustrative estimate only. Actual cavity pressure depends on resin, flow path, gate, wall thickness, fill speed and packing. Use mould-flow analysis or validated process data when available.

## Slide 9
5. Choosing the number of cavities
PRODUCTIVITY
09
• Estimate demand, annual production hours and target cycle time
• Check shot capacity and clamp force for the proposed cavity count
• Confirm platen size, tie-bar spacing and mould envelope
• Balance runner layout, filling and cooling between cavities
• Consider tool cost, maintenance, reject rate and changeover needs
Demand-based estimate
Required parts/hour = demand ÷ planned production hours
Cavities needed ≈ parts/hour × cycle time (s) ÷ 3,600
Round up only after checking the machine, tooling and economics. Add planned uptime and scrap assumptions separately.

## Slide 10
6. Shot capacity & machine fit
MACHINE SIZING
10
• Compare total shot mass with the machine's rated shot capacity
• Use the resin-specific capacity basis (often PS-equivalent) carefully
• Check injection pressure at the required flow rate—not just the maximum label
• Verify screw recovery time, cushion, plasticising capacity and residence time
• Confirm mould height, opening stroke, daylight and ejector stroke
Shot utilisation
Shot utilisation (%) = required shot mass ÷ rated usable shot mass × 100
Use the machine maker's guidance for the preferred operating range.
Too small: unstable filling or insufficient shot. Too large: long residence time or poor process control.

## Slide 11
7. Runner, sprue & gate calculations
FEED SYSTEM
11
Runner volume (circular)
V = π × d² ÷ 4 × L
For multiple runner segments, calculate each segment and add volumes. Convert units consistently.
Gate design checks
Balance gate size, shear heating, freeze-off, vestige, packing and cosmetic needs.
Gate dimensions are validated by resin data, flow analysis and trials.
A simple volume estimate helps shot sizing, but runner/gate sizing cannot be safely finalised from one universal formula. Consider pressure drop, shear rate, gate seal time, weld lines and cavity balance.
Hot runner: include manifold/nozzle layout, thermal balance and maintenance access.

## Slide 12
8. Injection pressure & filling
PROCESS WINDOW
12
Key idea
Machine injection pressure must overcome pressure losses through the nozzle, sprue, runner, gate and part flow path.
Check these factors
Resin viscosity • wall thickness • flow length • fill speed • gate size • melt temperature • venting
Do not equate hydraulic pressure, specific injection pressure and cavity pressure without checking the machine's pressure intensification ratio and measurement basis. Use machine documentation and cavity-pressure data where available.
Use a short-shot study and process monitoring to validate the filling profile.

## Slide 13
9. Cooling time: first estimate
THERMAL DESIGN
13
Simplified plate estimate
For a flat plate, a common first approximation is:
t ≈ (s² / (π² α)) × ln[ (4/π) × (Tm − Tw)/(Te − Tw) ]
Symbols
s = wall thickness (m)
α = polymer thermal diffusivity (m²/s)
Tm = melt temperature; Tw = mould-wall temperature; Te = ejection temperature
This idealised relation assumes simplified geometry and boundary conditions. Real cooling depends on geometry, crystallinity, contact, cooling-channel placement and ejection stiffness; use simulation and trial measurements for final cycle time.
Cooling is often a major contributor to total cycle time.

## Slide 14
10. Cooling heat-load estimate
THERMAL DESIGN
14
Polymer heat removed
Q̇ ≈ m × Δh ÷ cycle time
m = polymer mass per cycle; Δh = enthalpy removed per unit mass (use resin data).
Coolant heat balance
Q̇ = ṁwater × cp × ΔTwater
cp water ≈ 4.18 kJ/(kg·K) near room temperature.
Compare the heat-load estimate with cooling-system capacity and measured inlet/outlet temperatures. Flow rate alone does not guarantee performance; turbulent flow, channel layout, scale and circuit balance matter.
Use appropriate units and a consistent time basis.

## Slide 15
11. Cooling-channel design checks
THERMAL DESIGN
15
• Keep channel distance and spacing consistent where geometry permits
• Avoid channels too close to cavity surfaces or thin steel sections
• Check pressure drop, flow balance, fittings and leak risk
• Use baffles, bubblers or conformal channels only when justified
• Measure each circuit's flow and inlet/outlet temperature
Reynolds number
Re = ρ v D ÷ μ
ρ = coolant density; v = mean velocity; D = hydraulic diameter; μ = dynamic viscosity.
Higher Reynolds number generally indicates stronger mixing; use a cooling-design reference and supplier limits to set target flow.

## Slide 16
12. Total cycle-time model
PRODUCTIVITY
16
Cycle-time components
Total cycle ≈ fill + pack/hold + cooling + mould open/eject + mould close
Some machine actions overlap; avoid double-counting.
Output estimate
Parts/hour = cavities × 3,600 ÷ cycle time (s)
Example: 2 cavities, 30 s cycle = 240 parts/hour before downtime and rejects.
Real output depends on uptime, changeovers, scrap, operator handling, robot time, material drying and quality checks. Use OEE or a plant-specific availability factor for planning.

## Slide 17
13. Draft, ejection & release checks
TOOL DESIGN
17
• Draft angle depends on texture, depth, resin and surface finish
• Provide uniform, well-supported ejector contact where possible
• Avoid ejector pins on fragile or highly cosmetic surfaces
• Check core pull, slides, lifters and undercut release sequence
• Estimate ejection force only with realistic friction and contact data
Ejection force concept
F ≈ friction coefficient × normal contact force
This is a conceptual relation—not a universal mould-sizing equation.
Use part geometry, shrink-on-core behaviour, surface finish and resin-specific trials to determine the actual release requirement.

## Slide 18
14. Venting & air-trap checks
TOOL DESIGN
18
Why venting matters
Trapped air can cause burns, short shots, poor weld lines and unstable filling.
Design approach
Place vents at last-to-fill regions and likely air traps. Vent depth and land length depend on resin and supplier guidance.
Vent dimensions are material-sensitive: too shallow can block flow; too deep can flash. Use the resin supplier's recommendations, moulding references and controlled trial adjustments.
Do not use a single vent-depth value for every polymer.

## Slide 19
15. Mould steel & tool-life factors
TOOL MATERIALS
19
• Select steel by expected shots, resin abrasiveness and corrosion risk
• Consider polishability, hardness, toughness and machinability
• Use corrosion-resistant grades where resin or coolant chemistry demands it
• Match inserts and wear components to expected maintenance strategy
• Confirm heat treatment, surface treatment and supplier certificates
Typical decision factors
Production volume • glass-filled resin • texture / polish • corrosion • repair strategy • budget
Steel selection is not a calculation alone. Use a toolmaker's material specification and documented hardness targets.

## Slide 20
16. Tolerances & tool correction
QUALITY
20
Tolerance stack-up
Identify critical dimensions, datum scheme, GD&T, assembly function and measurement method before cutting steel.
Correction loop
Tool trial → measure parts → compare to drawing → separate shrinkage / process / tool effects → correct and revalidate.
Do not automatically compensate every out-of-tolerance dimension by changing the cavity. Process settings, moisture, conditioning, temperature and measurement technique can also shift dimensions.

## Slide 21
17. Quick formula reference
REFERENCE
21
Calculation | Formula / relationship | Units
Part mass | Volume × density | g or kg
Shot mass | Parts mass + cold runner / sprue mass | g or kg
Clamp force | Projected area × cavity pressure | N, kN, tonne-force
Parts/hour | Cavities × 3,600 ÷ cycle time | parts/h
Runner volume | π × d² ÷ 4 × length | mm³ or cm³
Coolant heat rate | Mass flow × cp × coolant ΔT | W or kW
Reynolds number | ρ × velocity × hydraulic diameter ÷ viscosity | dimensionless
Shrinkage estimate | Mould size ≈ part size ÷ (1 − shrinkage) | mm

## Slide 22
18. Integrated example: 4-cavity part
WORKED EXAMPLE
22
Part & resin
Part volume: 42 cm³
Density: 1.05 g/cm³
Part mass: 44.1 g
Shot estimate
4 × 44.1 g = 176.4 g
Cold runner: 18 g
Total shot ≈ 194.4 g
Clamp estimate
Projected area total: 320 cm²
Assumed cavity pressure: 35 MPa
Force ≈ 1,120 kN ≈ 114 tf
Next checks: machine usable shot capacity, clamp rating with justified margin, tie-bar spacing, injection pressure, runner balance, cooling time and dimensional capability.
Illustrative numbers only. Do not use as a released production design.

## Slide 23
19. Defects: what to check first
PROCESS TROUBLESHOOTING
23
Short shot
Filling pressure/speed, venting, gate restriction, melt temperature
Flash
Clamp force, parting-line damage, pressure, viscosity, mould alignment
Sink / voids
Wall transitions, packing pressure/time, gate seal, cooling
Warp / dimension shift
Cooling balance, material shrinkage, fibre orientation, packing
Burn marks
Air traps, venting, fill speed, decompression / process profile
Weld lines
Gate location, flow-front temperature, venting, filling pattern

## Slide 24
20. Pre-release design checklist
QUALITY GATE
24
• Part data and resin grade are confirmed
• Shrinkage assumption is documented
• Cavity count and layout are balanced
• Clamp force and shot capacity are checked
• Runner, gate and vent concepts are reviewed
• Cooling circuits and heat load are assessed
• Draft, undercuts and ejection sequence are checked
• Steel, hardness and tool-life requirements are specified
• Critical dimensions and measurement plan are agreed
• Machine envelope and safety clearances are verified
• Trial plan and acceptance criteria are documented
• Calculations are reviewed and revision-controlled

## Slide 25
Engineering references & disclaimer
FINAL NOTES
25
• Use the exact polymer supplier datasheet and processing guide
• Use the injection-moulding machine maker's specifications
• Use recognised plastics processing / mould design references
• Use CAD measurement, mould-flow analysis and trial data where appropriate
• Record assumptions, units, revision and reviewer for every calculation
Important disclaimer
This educational toolkit provides preliminary estimation methods. It is not a certified design, and it does not replace qualified engineering review, simulation, machine-maker limits, safety requirements or production validation.
Marketing note: customise the cover with your brand, logo, contact details and edition number before selling.

## Slide 26
ENGINEERING KNOWLEDGE • PRACTICAL CALCULATIONS
DESIGN SMARTER.
CALCULATE WITH CONFIDENCE.
Injection Mould Design & Calculations — A–Z Toolkit
• Core formulas and worked examples
• Machine sizing, runners, cooling and quality checks
• A practical starting point for students and junior engineers
ADD YOUR BRAND / PAGE NAME / CONTACT HERE