## Slide 1
PRACTICAL INJECTION MOULDING GUIDE
MOULDING DEFECTS
& TROUBLESHOOTING
Causes • Prevention • Corrective actions
A practical reference for students, operators and junior engineers
CAD & MANUFACTURING | EDUCATIONAL EDITION
IDENTIFY → CHECK → CORRECT

## Slide 2
How to troubleshoot a moulding defect
START HERE
02
1. Observe
Record defect location, frequency, machine settings and material lot.
2. Check causes
Change one factor at a time. Check material, tool, machine and process.
3. Verify
Run a controlled trial and confirm part dimensions, appearance and repeatability.
Troubleshooting rule: do not randomly increase temperature, pressure or speed. First confirm the defect, establish a stable baseline, and change one parameter at a time.
Safety: follow machine lockout and guarding procedures. Never reach into a running machine or hot mould.

## Slide 3
Common injection moulding defects
DEFECT OVERVIEW
03
Short shot
Part is incompletely filled
Flash
Thin excess plastic at the parting line
Sink marks
Local depressions on the surface
Voids
Internal cavities inside thick areas
Warping
Part bends or twists after moulding
Burn marks
Brown/black marks from trapped gas or overheating
Weld lines
Visible line where flow fronts meet
Splay / silver streaks
Streaks from moisture, gas or degradation
Jetting
Snake-like flow marks near the gate
Ejector marks
White spots or impressions from ejection
Bubbles
Gas pockets or surface blisters
Dimensional variation
Part size changes from shot to shot

## Slide 4
1. Short shot
DEFECT GUIDE
04
What you see
The cavity is not completely filled; the part may have missing edges, ribs or thin sections.
Likely causes
• Insufficient shot size or fill time
• Low melt / mould temperature or excessive viscosity
• Restricted gate/runner, poor venting or excessive flow length
• Injection pressure or speed limit reached
Corrective actions
• Confirm material is dried as specified and shot size is correct
• Check gate/runner restrictions and vents
• Review fill speed, melt temperature and mould temperature within supplier limits
• Check machine pressure limits and transfer position; use a short-shot study
Do not raise pressure blindly—check tool restrictions and machine limits first.

## Slide 5
2. Flash
DEFECT GUIDE
05
What you see
Thin excess plastic escapes at the parting line, inserts or slides.
Likely causes
• Insufficient clamp force or uneven clamping
• Damaged, dirty or worn parting surfaces
• Excessive cavity pressure, overpacking or low melt viscosity
• Mould misalignment or unsupported steel
Corrective actions
• Inspect and clean the parting line after safe shutdown
• Check mould alignment, support and wear
• Review fill/pack profile and transfer point
• Verify clamp force against projected area and actual process pressure
Do not simply increase clamp tonnage; excessive clamp force can damage the tool.

## Slide 6
3. Sink marks
DEFECT GUIDE
06
What you see
Surface depressions commonly appear over ribs, bosses or thick sections.
Likely causes
• Thick-to-thin wall transitions
• Insufficient packing pressure/time
• Gate freezes before the section is packed
• Uneven cooling or excessive local material volume
Corrective actions
• Improve wall uniformity and core out thick sections where design allows
• Optimise packing pressure/time using a gate-seal study
• Check gate size/location and cooling balance
• Confirm resin-specific processing window
Sink marks are often a design + packing + cooling issue; changing only temperature may not solve them.

## Slide 7
4. Voids
DEFECT GUIDE
07
What you see
Internal cavities form inside thick sections; some may not be visible externally.
Likely causes
• Insufficient packing of the core of thick sections
• Premature gate freeze-off
• Local shrinkage as material cools
• Entrapped gas or material-related issues
Corrective actions
• Inspect sectioned samples or use suitable inspection methods
• Review wall thickness and packing profile
• Check gate seal time and gate design
• Confirm material condition and mould temperature
Do not assume every void is a gas bubble; shrinkage voids and gas-related voids need different fixes.

## Slide 8
5. Warping
DEFECT GUIDE
08
What you see
The part bends, twists or changes shape after ejection or conditioning.
Likely causes
• Uneven cooling across the part
• Non-uniform shrinkage or fibre orientation
• Unbalanced packing / gate placement
• Ejection while the part is too hot or poorly supported
Corrective actions
• Balance cooling circuits and verify actual flow
• Review gate position, wall thickness and rib layout
• Optimise packing and cooling time
• Improve ejection support; measure after a defined conditioning period
Check dimensions after consistent conditioning; hot parts may distort after ejection.

## Slide 9
6. Burn marks
DEFECT GUIDE
09
What you see
Brown or black discoloration, often at end-of-fill areas or trapped-air locations.
Likely causes
• Trapped air compressed rapidly (diesel effect)
• Poor venting or blocked vents
• Excessive fill speed in a trapped-air region
• Material degradation from excessive temperature or residence time
Corrective actions
• Clean and inspect vents; add/relocate vents only after tool review
• Optimise fill speed near end-of-fill
• Check melt temperature and residence time
• Confirm material drying and purge practice
Burn marks can indicate compressed trapped gas; do not treat them only as a temperature problem.

## Slide 10
7. Weld lines
DEFECT GUIDE
10
What you see
A line or weak seam forms where two melt fronts meet around a hole or flow split.
Likely causes
• Low flow-front temperature
• Poor gate location or flow balance
• Insufficient venting at the meeting point
• Contamination or inadequate packing
Corrective actions
• Review gate location and flow path with mould-flow analysis if available
• Optimise melt/mould temperature within grade limits
• Improve venting and flow-front meeting conditions
• Assess strength and cosmetic requirements at the weld line
Do not promise that all weld lines can be eliminated; placement and strength may be the design goal.

## Slide 11
8. Splay / silver streaks
DEFECT GUIDE
11
What you see
Silvery lines or streaks follow the flow direction on the part surface.
Likely causes
• Moisture in hygroscopic resin
• Air entrainment or decompression issues
• Thermal/shear degradation or contamination
• Incorrect drying, storage or handling
Corrective actions
• Verify dryer temperature, time and dew point against resin supplier guidance
• Check material storage and sealed transfer
• Review screw recovery, back pressure and decompression settings
• Purge and inspect for contamination or degradation
Drying conditions vary by resin grade; do not apply one temperature/time to all polymers.

## Slide 12
9. Jetting
DEFECT GUIDE
12
What you see
A snake-like or worm-like surface mark appears near the gate.
Likely causes
• Melt jet travels freely into a larger cavity before attaching to the wall
• Gate directs flow too quickly into open space
• High initial injection speed or unsuitable gate geometry
Corrective actions
• Review gate type, position and direction
• Use a controlled slower initial fill stage if suitable
• Encourage flow to attach to the cavity wall
• Confirm changes do not create short shots or weld-line problems
Gate changes require toolmaker review and a controlled process trial.

## Slide 13
10. Ejector marks / whitening
DEFECT GUIDE
13
What you see
White spots, stress marks or pin impressions appear after ejection.
Likely causes
• High ejection force or insufficient draft
• Part too hot or stuck on the core
• Ejector pins too small or poorly positioned
• Surface texture, undercuts or uneven shrinkage increase drag
Corrective actions
• Confirm adequate draft and smooth release surfaces
• Balance ejector layout and contact area
• Optimise cooling before ejection
• Inspect for undercuts, damage and core surface issues
Check pin layout and tool condition before changing ejection pressure.

## Slide 14
11. Bubbles / blisters
DEFECT GUIDE
14
What you see
Gas pockets, bubbles or raised blisters appear inside or on the surface.
Likely causes
• Moisture or volatile release from resin
• Trapped air or poor venting
• Excessive melt temperature or residence time
• Local overheating or contamination
Corrective actions
• Check resin drying and storage requirements
• Inspect vents and material cleanliness
• Review melt temperature and residence time
• Compare defect location with flow path and thick sections
Use cross-section inspection when needed to distinguish internal voids from surface blisters.

## Slide 15
12. Dimensional variation
DEFECT GUIDE
15
What you see
Critical dimensions vary between shots or drift over a production run.
Likely causes
• Unstable melt / mould temperatures or cooling
• Inconsistent packing, cushion or transfer point
• Material lot, moisture or regrind variation
• Measurement method or conditioning differences
Corrective actions
• Stabilise the process and monitor temperatures
• Check cushion, transfer and packing repeatability
• Control material lot, drying and regrind ratio
• Use a consistent measurement method and sampling plan
Separate process variation from tool dimensions before cutting or modifying steel.

## Slide 16
13. Flow lines
DEFECT GUIDE
16
What you see
Flow-like bands or colour/texture differences appear on the surface.
Likely causes
• Uneven flow speed or temperature
• Wall thickness changes or flow obstruction
• Gate location and surface finish
• Pigment or material mixing variation
Corrective actions
• Review fill profile and melt/mould temperature within limits
• Improve flow path and wall transitions where feasible
• Check gate position and material mixing
• Compare defect location across cavities
Validate each change with a controlled trial and record the result.

## Slide 17
14. Gate blush / halo
DEFECT GUIDE
17
What you see
A cloudy ring or blush appears around the gate area.
Likely causes
• High shear or excessive speed at gate
• Gate geometry too small or sharp
• Melt / mould temperature mismatch
• Material degradation or stress concentration
Corrective actions
• Review initial injection speed and gate design
• Check gate dimensions and edge condition
• Confirm material processing window
• Validate appearance after controlled trials
Validate each change with a controlled trial and record the result.

## Slide 18
15. Delamination
DEFECT GUIDE
18
What you see
Thin layers peel or separate from the surface.
Likely causes
• Material incompatibility or contamination
• Moisture or volatile contamination
• Excessive shear or degraded material
• Poor mixing or unsuitable regrind combination
Corrective actions
• Check resin identity, colourant and regrind compatibility
• Verify drying and material handling
• Purge and inspect screw/nozzle for contamination
• Consult the resin supplier before changing process settings
Delamination may indicate material incompatibility; process changes alone may not correct it.

## Slide 19
A practical troubleshooting sequence
SHOP-FLOOR METHOD
19
A
Identify defect + location
B
Check material, drying and lot
C
Check tool: gate, vents, parting line, cooling
D
Check machine: shot, pressure, clamp, repeatability
E
Change one setting within approved limits
F
Run trial, measure, document and standardise

## Slide 20
Process parameters: what each one influences
PROCESS BASICS
20
Parameter | Potential influence (not a one-to-one fix)
Melt temperature | Viscosity, flow, degradation, surface appearance
Mould temperature | Surface finish, weld lines, shrinkage, cycle time
Injection speed | Flow-front behaviour, shear, jetting, trapped-air risk
Injection pressure | Ability to fill; must remain within machine/material limits
Packing pressure/time | Sink, voids, weight and dimensions
Cooling time / flow | Ejection stability, warpage, cycle time
Back pressure / screw speed | Mixing, melt quality, shear and recovery
Decompression | Can affect drooling, air ingestion and splay

## Slide 21
Worked troubleshooting example: sink marks
CASE STUDY
21
Observation
Sink marks appear above thick ribs on a cosmetic part.
Investigate
Compare wall thickness, gate seal time, packing profile and cooling balance.
Trial plan
Change one factor at a time; weigh parts and inspect the same locations.
Possible sequence: confirm the gate has not frozen too early → test packing time in small increments → verify weight stabilises → inspect sink depth → confirm dimensions and ejection stability.
If packing changes do not help, review rib thickness, gate location and cooling—not just machine settings.

## Slide 22
Defect-prevention checklist
QUALITY CONTROL
22
• Use the correct resin grade and colourant
• Dry and store material to supplier requirements
• Keep vents, gates and parting surfaces clean
• Verify cooling flow and mould temperature
• Use a documented start-up and stabilisation procedure
• Track cavity-wise defects and part weight
• Change only one process variable per trial
• Record settings, lot number, time and defect rate
• Use agreed inspection methods and conditioning
• Maintain machine and mould on a planned schedule
• Escalate recurring defects to process/tooling engineers
• Revalidate after material, tool or process changes

## Slide 23
CAD & MANUFACTURING • ENGINEERING LEARNING SERIES
FIND THE DEFECT.
FIX THE ROOT CAUSE.
Injection Moulding Defects & Troubleshooting
• 15+ common defects explained
• Causes, prevention and corrective actions
• Practical shop-floor troubleshooting workflow
ADD YOUR LOGO • BRAND NAME • CONTACT DETAILS

## Slide 24
Important technical notes
REFERENCE & DISCLAIMER
24
• Defects can have multiple causes; location and timing are useful clues.
• Processing recommendations must follow the exact resin supplier's guidance.
• Machine-specific limits, tooling condition and part design must be considered.
• Validate corrective actions with controlled trials and documented inspection.
• Use qualified engineering review for production-critical changes.
Educational use
This deck is a troubleshooting guide, not a universal recipe. Do not apply numerical settings without resin-, machine- and tool-specific validation.
Prepared as an editable teaching / marketing PPT. Add your brand and review technical content before commercial sale.